| Calcium Hypochlorite |
| --- |
| DESCRIPTION |
| In 65% and 70% sales grade specification |
| Physical Properties |
| Molecular Weight | 142,98 |
| Specific Density | 2,35 |
| pH (Sol. 1%) |  |
| Deteriorates Above | 177 ºC |
| Chemical Composition |
| Chemical Formula | Ca(OCl)2 |
| Chlorine content | 70% |
| Fe | 0,03% max |
| Mn | 40 ppm max |
| Water Insolubles (%) | 18% max |
| Moisture | 5 - 10% |
| Packaging |
| 50 kgs in iron drum (65% grade) | Standard |
| 40 kgs in plastic drum (70% grade) | Standard |
| Validity |
| One Year if properly storage in a dry warehouse |
| The Registry of Toxic Effects of Chemical Substances |
| CAS No: 7778-54-3 |